## Slide 1: Carbonate-hosted Pb-Zn-(Ba-F) deposits of the Alpine-type in the Eastern and Southern Alps
Frank Melcher
Montanuniversität Leoben, Austria
IAEG 50th Anniversary Conference
Sept 9, 2023
MU Leoben: Viktor Bertrandsson Erlandsson, Veronika Gartner, Elisabeth Henjes-Kunst, Johann Raith, Gerd Rantitsch, Peter Onuk
BGR Hannover: Friedhelm Henjes-Kunst
University of Ljubljana: Barbara Potočnik Krajnc, Aleš Šoster

## Slide 2
Interactive Raw Material Information System (Geosphere Austria): 455 Pb-Zn „deposits“ in Triassic carbonates (Austria)
Vienna
Munic
Lake Constance
Graz
Leoben
100 km
Salafossa
Bleiberg
Raibl
Mežica

## Slide 3
Interactive Raw Material Information System (Geosphere Austria): 455 Pb-Zn „deposits“ in Triassic carbonates (Austria)
Vienna
Munic
Lake Constance
Graz
Leoben
100 km
Salafossa
Bleiberg
Raibl
Mežica

## Slide 4
Mine | Country | Host rock | Resource | Grade | Production | Activity
Bleiberg-Kreuth | A (Carinthia) | Carn | 43 Mt (3.5 Mt metal) | 1.1% Pb, 5.9% Zn | 2.2 Mt metal | 1333-1994
Raibl | Italy | Carn | 18 Mt | 1.2% Pb, 6.0% Pb | 1.5 Mt metal | 14th-1991
Mežica | Slovenia | Carn | 34 Mt | 2.4% Pb, 3.4% Zn | 1.5 Mt metal | 1424-1993
Salafossa | Italy | Carn | 10 Mt | 0.95% Pb, 4.9% Zn | 0.5 Mt metal | 1957-1986
Gorno | Italy | Carn | 6 Mt | 3.5% Zn cut-off |  | -1980s
Lafatsch | Austria (Tyrol) | Carn | 4 Mt(?) (0.6 Mt prov) | 1.6% Pb, 6.2% Zn |  | -1550 (1963)
Silberleiten | Austria (Tyrol) | Carn |  |  |  | 15th-1921
Argentiera | Italy | Anis |  | 1% Pb, 6% Zn | 1 Mt ore | -1971
Topla | Slovenia | Anis |  | 3.3% Pb, 10% Zn | 0.25 Mt ore | 1974-1988
Hochobir | A (Carinthia) | Carn | 0.3 Mt |  |  | MA
Radnig | A (Carinthia) | Carn | 0.2 Mt |  |  | -ca. 1900
Jauken | A (Carinthia) | Carn | 0.05 Mt |  |  | -ca. 1900
Rauschberg | Germany | Carn |  |  |  | 1636 - 1894
Carbonate-hosted Pb-Zn deposits in Mesozoic host rocks
  Total of 510 APT occurrences in Austria (89%), Italy (6%), Slovenia, Switzerland and Germany (<2% each)

## Slide 5: Research question
Despite representing important mining districts until the 1990s, >200 years of scientific research have not been enough to fully understand these deposits and reach an accepted deposit model
APT versus MVT versus IRT
Deposit models range from syngenetic to epigenetic with or without magmatic influence
Age estimates ?
Triassic (Middle or Upper)
Jurassic
Cretaceous
Oligocene
Miocene
telemagmatic genesis
Lateral secretionary processes
secondary hydrothermal processes
Volcanogenic-exhalative
Super- and submarine weathering
Sabkha process
karst systems
weathering debris of non-ferrous metal mineralisations
formation waters

## Slide 6: Bleiberg – type locality of APT
Erich Schroll (1923 – 2008)

## Slide 7
Lafatsch
Gorno
Salafossa
Bleiberg
Raibl
Mezica
Tectonic map

## Slide 8
Lafatsch
Gorno
Salafossa
Bleiberg
Raibl
Mezica
Stratigraphic map
Drau – Karawanken Range

## Slide 9: Pb-Zn distribution in the Drau and Karawanken Range
Bleiberg
Mezica
Carn
Carn
Anis
Anis
Nor

## Slide 11
Pirkach, Mühlenstollen
Jauken South slope
Hochobir
Jauken North

## Slide 12
Dobratsch (2160m)
Gail valley (550m)
Drau valley (500m)
Gummern
Villach
Arnoldstein (former metallurgical plant)
Erzbergrücken (1500-1700m)
Bleiberg valley (900m)
Medieval
Hoffnungsgebiet
19-20th
5 km

## Slide 13
Dumps from Medieval mining
Zn-Pb-Mo, Ge?
Flotation tailings
Bleiberg-Kreuth, Carinthia
Pb-Zn mining until 1993 (BBU)
By-products cadmium, germanium

## Slide 14: Medieval mine dumps COMMBY project MSc thesis S. Dollinger 2022

## Slide 15: Mineralogy of waste rock dumps
Pb cerussite
anglesite
galenite
Zn smithsonite
hemimorphite
fraipontite
limonite
(sphalerite)
Mo wulfenite
limonite
Barite
Fluorite
pXRF result | wt%
Pb | 0.3
Zn | 0.54
Mo | 0.09

## Slide 16: Zn-Pb-Mo content in waste rock dumps
Marousek et al. 2023

## Slide 17: Multi Metal Development (Canada)
Bleiberg Project - Multi-Met (multimetdev.com)
Multi Metal Development Limited (MultiMet) (formerly American CuMo Mining Corporation) is a Canadian-based mining company ….
MultiMet is currently advancing two projects— …. and its newly-acquired Bleiberg Project in Austria. ….
(101 licences)
October 26, 2022 MultiMet announced the signing of a joint venture agreement for the development of the Bleiberg Project, with Battery Age Metals (formerly Pathfinder Resources Ltd.) an Australian public company.
Mining licences:

## Slide 18: Multi Metal Development (US)

## Slide 19: Multi Metal Development (Canada)

## Slide 20
Six ore horizons
Highest Pb-Zn in upper Wetterstein Formation
Various ore textures
  layers
  veins
  breccia
  Vein networks
Modified from Cerny (1989) and Schulz & Schroll (1977)
Bleiberg-Kreuth, Carinthia
>3 million tons of metal at Zn/Pb = 5-6
Germanium, cadmium, molybdenum as by-products
ca. 200 g/t Ge and 2000 g/t Cd hosted by sphalerite
Smelter nearby (Arnoldstein)
Notes: Erwähnen, dass auch in der anisischen Lage Pb-Zn vorkommt
Wettersteinkalk: Bleiberger Sonderfazies -lagunare Fazies mit 9 Emersionshorizonten an denen die Vererzung gebunden ist. Crest unklar was genau -evtl Riff?! Unterschiede in der Lagerstätte von West nach Ost.
Typuslokalität für Alpine Pb-Zn-LS --> MVT und SEDEX-Kram erwähnen:
Sedex: Sedex
Syndiagenetische/synsedimentäre Bildung
Massive polymetallische Buntmetallvererzungen (Cu-Pb-Zn) in marinen Sedimenten
Stratiforme Lagerstätten, z.B. Broken Hill (Australien), Rammelsberg (Deutschland)
auch SMS (massive Sulfidlagerstätten), Terminus ist veraltet. Sulfidlagerstätten in marinen Sedimenten/ Stratiform, große laterale Ausdehnung, laterale Cu-Pb-Zn- und vertikale Cu-Zn-Pb-Zonierung
Hauptmineralisation: Sphalerit, Galenit, Baryt, Kupfer und Silber. Feinkörnige und geschichtete Erze. Erze werden aus heißen (100-300°C) Fluiden gefällt durch Reduktion der Metalle mit Schwefel.
MVT: Epigenetische Bildung
Schichtgebundene Pb-Zn-(Ba-F)-Lagerstätten in Karbonaten
Vererzung sowohl in Schichten als auch in Gängen/Adern
z.B. Virburnum Trend (USA) Sulfidlagerstätten, die große Erzdistrikte in Plattformkarbonaten bilden. Stratiforme Vererzung in Schichten, Adern, Brekzien, etc. Meist grobkörniges Erz.
Einfache Mineralogie (Sphalerit mit wenig Fe, Galenit mit wenig Ag, Fluorit, Baryt, Cc, Dol). Vererzung sind v.a. epigenetische Hohlraumfüllungen. Erze werden durch Reduktion mit Schwefel aus moderat warmen (80-220°C) Fluiden gefällt.

## Slide 21
Antoni
Rudolf
Stefanie
Franz-Josef
Pb:Zn
1:1
1:2
1:6 to 1:4
1:2

## Slide 22: Tectonic structure of the Bleiberg deposit

## Slide 23: Bleiberg, Antoni Schacht, Bereich Max

## Slide 24: Maxer Bänke mineralization (lowermost ore horizon)

## Slide 25: Stollenwanderweg Bleiberg: historical mine trail

## Slide 26
Reconstruction of the Bleiberg mineralization during the Carnian

## Slide 27: Lead horizons in the upper Wetterstein limestone

## Slide 28
Barite
Ga
Sph + Fluorite
Fluorite
Erzkalk, Wetterstein limestone, Grube Rudolf, Bleiberg
Ore sediment, spatially-rythmic, fine-grained, partly collectively crystallised, calcareous mud,
“Bodenerz”
(Schroll 2008)
Schalenblende
Sph

## Slide 30: „Erzwannen“ (Ore troughs)

## Slide 31: Microbial textures in sphalerite ores from Bleiberg, Crest horizon (“Kalkscholle”).
Photo: H. Kucha
Massive sphalerite ore, Crest horizon (Schwellenfazies).
Dark brown sphalerite bands have been interpreted as mineralized microbial mats.
Anhydrite

## Slide 32
(A, B) Sphalerite band formed by replacement of former microbial mat. The band consists of circular biogenic (?) globules with core and rim (C, R).
Reflected light,
with crossed polars.
FE-SEM image of etched cavity within micro-globular sphalerite showing nano-globules of sphalerite.
FE-SEM image showing details of (C) with ZnS nano-globules and part of a mineralized bacterial filament. Photos H. Kucha.
Kucha et al. (2003, 2010)
Microbial textures in sphalerite ores from Bleiberg, Crest horizon (“Kalkscholle”).

## Slide 33: Cave del Predil (Raibl)
Jadoul et al. (2002), ore bearing Schlern dolomite is marked in brown
VERONIKA GARTNER MSc thesis 2023c

## Slide 34
Map of the Raibl mine in 1903, from Göbl (1903),
three color varieties of colloform sphalerite
Cave del Predil (Raibl)
VERONIKA GARTNER MSc thesis 2023c

## Slide 35
Röhrenerz (tubular ore)
Raibl deposit, ore textures
Stalactitic/Dendritic ore
Schalenblende
Granular ore
V. GARTNER (2023)
Posepny 1873
10-16 cm long tubes

## Slide 36: Mežica Pb-Zn mine
BARBARA POTOČNIK KRAJNC, MSc thesis 2021

## Slide 37
A schematic cross-section through the Naveršnik mining area, Mežica deposit, showing the main geological features and distribution of mineralisation. Modified after Zorec (1955).
BARBARA POTOČNIK KRAJNC, MSc thesis 2021

## Slide 38: Mežica deposit, ore textures
Ore rhythmite
Breccia and vein-type, replacement
Colloform sph in cockade breccia

## Slide 39
Brown colloform sphalerite type Sp1a, fragmented and subsequently cemented by sphalerite types Sp4a and Sp4b.
Vein-hosted ore, containing brown sphalerite Sp1b wrapped by colourless crystalline sphalerite Sp4a, and green crystalline sphalerite Sp4b.
Breccia ore containing unmineralised host-rock clast that is almost completely transformed into secondary hydrothermal dolomite. Colloform sphalerite type Sp1d and crystalline sphalerite type Sp2 form matrix and corrode galena.
Open space filled with colloform sphalerite Sp1. Open space was reactivated during later hydrothermal processes, reflected in the precipitation of saddle dolomite and marcasite.
Hand-specimen of sphalerite type Sp1c, which consists of a few cm thick spheroidal and irregularly shaped aggregates with differently coloured alternating bands, forming cockade texture.
BARBARA POTOČNIK KRAJNC, MSc thesis 2021

## Slide 40
Kuhlemann et al., Econ Geol 96 (2001)

## Slide 41: Trace element analysis of sphalerite (ppm)
Mn
Fe
Cu
Ga
Ge
As
Ag
Cd
Sn
Sb
Tl
Pb
Element | Md (max) | Element | Md (max)
Mn | 5,5 (1100) | Ag | 1,1 (44)
Fe | 2409 (3.5%) | Cd | 2509 (5515)
Cu | 136 (813) | Sn | 0,1 (1,9)
Ga | 2,2 (87) | Sb | 0,7 (499)
Ge | 196 (846) | Tl | 8 (179)
As | 51 (1122) | Pb | 311 (2860)
Median values of 14 deposits

## Slide 42
Trace elements and colour - Raibl/Cave del Predil
Mn
Cd
As
Fe
Ge
Tl
Pb
Red and brown sphalerite have elevated Fe, As, Ge, Tl and Pb

## Slide 43: Sphalerite trace elements of APT fit MVT box

## Slide 45
65°C
75°C
67°C
92°C
307°C
137°C
135°C
118°C
117°C
56°C
97°C
66°C
93°C
92°C
88°C

## Slide 46
Jauken
Bleiberg
Raibl
Fladung
Lafatsch
34S/32S in sphalerite (in-situ LA-QQQ-ICP-MS, Ounk 2018)
Sulphur isotope variation Bleiberg (Schroll 2006), bulk data
PbS
ZnS

## Slide 47
Henjes-Kunst, Boyce et al. 2017
Sulphur isotope variation in ore samples from Bleiberg deposit
Maxer Bänke horizon (Wetterstein limestone)
Erzkalk horizon (Wetterstein limestone)
Layered sph
-1.5 to -21 ‰
Schalenblende
-16 to -26 ‰
Galena
-21 to -22 ‰
ZnS I -6.6 ‰
ZnS II -6.6 ‰
ZnS IV -18.2 ‰
Schalenblende -22 ‰
Galena -7.7 to -25.1 ‰
Pyrite -21.8 ‰
Barite +17 ‰

## Slide 48
Sulphur isotopes and trace elements at the Bleiberg deposit

## Slide 49: Pb isotope signature of ore lead from APT deposits
DR Drau Range; Bb Bleiberg; NCA Northern Calcareous Alps; SCA Southern Calcareous Alps

## Slide 50: Rb-Sr dating of sphalerite from Bleiberg, Austria

## Slide 51: What has been dated at Bleiberg?
Crest ore
201 Ma
Cardita ore
229 Ma

## Slide 52: U-Pb dating of hydrothermal carbonate at Gorno, Italy
Giorno et al. 2022 Geology 50: 853-858

## Slide 53
Giorno et al. 2022 Geology 50: 853-858

## Slide 54: Paleogeographic reconstructions
modified after Haas et al. (2020)
Late Permian/Lower Triassic (A)
Late Jurassic (B)
Green circles indicate position of Upper Triassic APT occurrences in rocks of the Wetterstein Platform and the Raibl Group
Red circles indicate position of Middle Triassic (Anisian) APT occurrences overlying Lower Triassic clastic rocks

## Slide 55: Mineral deposits of Permo-Triassic age in the Alps
„Erzberg“ Siderite (500 Mt @ 33% Fe)
208 ± 22 Ma (Sm-Nd)
Breitenau magnesite
221 ± 16 Ma (Sm-Nd)
Hohentauern magnesite
285 ± 15 Ma (Sm-Nd)
LCT pegmatites
247-277 Ma

## Slide 56
Prochaska et al. 2014
Erzberg
Bleiberg
Seawater

## Slide 57
Burisch, Markl, Gutzmer 2022 EPSL

## Slide 58: Summary of APT deposits in the Eastern and Southern Alps
>500 Pb-Zn occurrences in 13 ore districts
Ores are restricted to Anisian and Carnian carbonate host rocks
Sphalerite is low in Fe, Mn, Co and In, but commonly contains elevated Cd, Ge, As, Tl and Pb, rarely also Ga and Ag
Sphalerite formation temperatures from 60 to 140°C
Galena is Ag-poor
Minor pyrite and marcasite display an As-Tl-(Hg) signature
Rb-Sr isochron dating of sphalerite at ≈229 Ma and at ≈207-201 Ma
Sulphur isotopes indicate bacteriogenic origin of sulphur, with minor thermogenic sources; barite shows seawater composition
Metal source from Paleozoic basement and pre-Triassic sedimentary rocks
Paleogeographic situation in an extensional/transtensional tectonic setting

## Slide 59: MVT vs APT
 | APT | MVT
Host rock | Shallow marine carbonate | Shallow marine carbonate
Age of host | Middle-Upper Triassic | Paleozoic
Mineralogy | Sph (Fe- poor), Ga, Ft, Ba, (Py, Mc) | Sph (Fe- poor), Ga, Py, Mc, (Ft, Ba)
Trace elements | Cd, Ge, As, Tl, (Ga) | Cd, Ga, Ge, (Cu), Ag, Ni, Co
Fluid salinity | 10-30% | 10-30%
Fluid temperature | 60-140°C | 75-200°C
Fluid origin | Evaporated seawater | Formation water + meteoric water
Depth | Shallow, surface | Deeper levels
Textures | Colloform, rythmites, bacteriogenic | Coarse rystalline to fine-grained
Sulphur | BSR dominant; -40 to 0 permil | TSR dominant, evaporites
Lead | B-type (>300 Ma) | J-type (model age younger than host rocks)
Age | Triassic, 230-200 Ma | Postdating host by x10 to x100 Ma
Tectonic setting | Extensional, transtensional | compressional

## Slide 60
„Good luck“